| http://www.ece.umd.edu/~pabshire/enee312h.htm | due Thursday, March 7, 2002 |
| --- | --- |

- Consider an abrupt p-n junction with Na = 5x1017 cm-3 and Nd = 1016 cm-3 at room temperature.

  - Find the ratio of the depletion region width on the n-side, xn, to the width on the p-side, xp.

  - Find the total width of the depletion layer (in microns).

  - Find the maximum electric field in this junction for applied biases of (i) VA=0 and (ii) VA=-12V.

  - The breakdown electric field in moderately doped silicon is approximately 5x105 V/cm.  At what reverse bias will the field reach this value, and what will the depletion region width be at that bias?

- Data from a measurement of the small-signal capacitance of a silicon p+-n diode structure as a function of bias voltage is plotted below in the form 1/Cdep2 versus Vab.  The area of the junction is 10-5 cm2.

  - What is the built-in potential of this junction?

  - What is the doping level of the more lightly doped side (n-side) of this diode in the vicinity of the junction?

  - What is the doping level of the more heavily doped side?

  - At some distance from the junction the doping level changes.

    - At what distance does the change occur?

    - Does the doping level increase or decrease at this point, and what does it become?

  - Suppose that in addition to the above structure there is a very heavily doped n+-region 3m from the junction.  How would you expect the plot of 1/Cdep2 versus Vab to look in this case?

- The short-circuited, symmetrically doped p-n diode shown below is illuminated by a distributed source that generates  hole-electron pairs/cm3 in the region .  You may assume: low level injection, ,, , .  Label sketches of the following over the range .

  - Find the total short-circuit current of the diode.

- –   7) Complete Sedra & Smith problems 3.47, 3.69, 3.71, 3.101

Design Question:

A photodiode has reverse saturation current IS = 1pA.  Upon illumination the short circuit reverse saturation current increases to about 1nA.  Compute the optimum load so that maximum power is delivered from the diode.